# Article Title

Author Name1, Author Name1,*, Author Name2

1Research Center for Chemistry, National Research and Innovation Agency (BRIN), Tangerang Selatan, KST BJ Habibie, Tangerang Selatan 15314, Indonesia

2Research Center for Environmental and Clean Technology, National Research and Innovation Agency (BRIN), KST Samaun Samadikun, Bandung 40135, Indonesia

*Corresponding author. E-mail: author@university.ac.id (Author Name)

# Abstract

A combination of doping and constructing a heterostructure is believed to be an effective strategy to decrease the band gap and enhance the charge separation efficiency of the SnO2 photocatalyst to make it suitable for pollution treatment under solar irradiation. In this study, Sn2+-SnO2 was combined with TiO2 to create a Sn2+-SnO2/TiO2 heterostructure using a sol-hydrothermal method.  XRD, SEM, TEM, Raman, XPS, and DR UV-Vis characterization showed that Sn(II) doped SnO2 with a particle size of 3.85 ± 0.85 nm formed a heterostructure with amorphous TiO2, narrowing the band gap down to 2.35 eV. Sn2+-SnO2/TiO2 exhibits better performance than Sn2+-SnO2, with kinetic constants 3.8 times higher for MO degradation and 2.2 times higher for Cr(VI) ion removal, respectively. Complete degradation of methyl orange (MO) was achieved within 20 minutes, while hexavalent chromium (Cr(VI)) was entirely reduced to trivalent chromium (Cr(III)) within 60 minutes under simulated solar light irradiation (λ ≥ 450 nm). The photocatalysis mechanism and the involved ROS were also investigated.

Keywords: Sn2+ self-doping, heterostructure, photocatalysis, Cr(VI) reduction, MO degradation

# Introduction

Water pollution caused by organic dyes and heavy metals, particularly hexavalent chromium (Cr(VI)), poses a significant environmental concern due to their persistence, toxicity, and resistance to natural degradation. Wastewater from textile, leather, and electroplating industries typically contains high levels of organic dyes and toxic metals such as Cr(VI), highlighting the need for environmentally friendly treatment methods. Advanced oxidation processes (AOPs) have emerged as promising approaches for removing persistent organic and inorganic pollutants. These methods—such as ozonation, Fenton reactions, and photocatalysis—rely on the generation of highly reactive species like hydroxyl radicals (•OH), which can effectively degrade complex pollutants [1,2].

Photocatalysis is a widely studied AOP that uses semiconductor materials to decompose organic pollutants and reduce heavy metal ions under light irradiation. Among the various photocatalysts, SnO2 has gained attention due to its abundance, low cost, and chemical stability [3–5]. Moreover, SnO2 can potentially be better than TiO2 because of its high electronic mobility, which is reported to be up to 100 times greater in ideal crystalline forms, which can contribute to improved charge transport [6,7].

However, the wide band gap of SnO2 (3.6 eV) limits its response to visible light, which constitutes the majority of solar radiation. To address this limitation, strategies such as doping and heterostructure formation have been proposed. Metal doping with Mn, Cr, Ni, Fe, Nb, Sb, and Ce [8–11] introduces impurity levels that narrow the band gap and improve charge separation. In addition to conventional doping, self-doping of SnO2 via Sn2+ substitution has recently emerged as an effective strategy to enhance visible-light activity. Incorporation of Sn2+ into the SnO2 lattice creates a new valence band above the O 2p orbitals, reducing the band gap and enabling photoresponse under lower-energy light [12]. For instance, Sn2+-doped SnO2 can oxidize pollutants under light with wavelengths >400 nm in just 15 minutes, with a photocatalytic activity 25 times higher than undoped SnO2 [13]. This enhancement is attributed to improved optoelectronic properties resulting from lattice distortion and the formation of oxygen vacancies upon Sn2+ introduction. These vacancies are critical in metal oxides, as they contribute to light absorption, charge separation, and act as active sites for adsorption and redox reactions—thereby enhancing the photocatalytic performance of SnO2 [14,15].

# Experimental

## 2.1 Materials

Titanium (IV) butoxide (TBT), tin (IV) chloride pentahydrate (SnCl4·5H2O), and tin (II) chloride dihydrate (SnCl2.2H2O) were selected as the precursors. All were purchased from Merck, Germany. Isopropyl alcohol, methyl orange, potassium dichromate, and hydrazine hydrate were also purchased from Merck, Germany. MilliQ water was used in all experiments. All chemicals were used as-received without further purification.

# Results and Discussion

## 3.1 XRD Analysis

XRD patterns of Sn2+-SnO2, Sn2+-SnO2/TiO2 and TiO2 are shown in Fig. 1a. The XRD pattern of Sn2+-SnO2 exhibits several distinct peaks at 26.5°, 33.8°, 37.9°, 51.6°, 61.8° and 65.3° which can be assigned to the (1 1 0), (1 0 1), (0 2 0), (2 1 1), (1 3 0) and (0 3 1) planes of the tetragonal SnO2 phase as reported in JCPDS No. 41-1445. No other peaks of other tin oxide polymorphs, such as SnO and Sn3O4, were observed. Thus, Sn2+-SnO2 is a pure SnO2 phase. On the other hand, the TiO2 sample has peaks at 2θ = 25.3°, 37.8°, 48.0°, 53.9°, 55.0°, 62.7°, 68.8°, 70.7°, and 75.0°, which can be assigned to the (0 1 1), (0 0 4), (0 2 0), (0 1 5), (1 2 1), (0 2 4), (1 1 6), (2 2 0), and (1 2 5) planes of the anatase TiO2 phase (JCPDS No.  21-1272). This means that TiO2, which was prepared without the SnO2 precursor, has been crystallized into the anatase phase during the synthesis, although calcination was not applied. In contrast, the XRD pattern of Sn2+-SnO2/TiO2 has no peaks that can be ascribed to anatase. However, the Ti molar composition is relatively high at 50 mol% (or Sn:Ti = 1:1). The absence of TiO2 crystals implies that it may be present in the amorphous state and that the SnO2 may have suppressed its crystal growth. However, there is a slight bulge at 2θ ≈ 48.0° that can be attributed to the (0 2 0) anatase peak as highlighted by the blue circle in Fig. 1b. The occurrence of a bulge rather than a peak may be an indication that the growth of TiO2 is inhibited by the formation of SnO2 [16]. Yang et al. (2020) reported that in black SnO2/TiO2, TiO2 crystallization was suppressed when the Sn:Ti ratio was 1:1 or higher, even after calcination at 550 °C, and this occurred only when Sn:Ti < 1:2 [17]. Similarly, Hirano and Kono (2011) observed that TiO2 crystals in SnO2-TiO2 solid solutions were formed only when the Ti content was 90 mol%  (Sn:Ti = 1:9) [18]. Meanwhile, this study used an Sn:Ti ratio 1:1 and omitted the calcination process to prevent the oxidation of Sn2+ to Sn4+. Another interesting observation is the peak broadening and shift to the higher angle of the (1 0 1) and (2 1 1) peaks of the rutile phase of SnO2 in Sn2+-SnO2/TiO2, as shown in Fig.  1b. The change in peak characteristics may be attributed to modifications in the crystal lattice structure due to the incorporation of Ti4+ into the SnO2 lattice [16]. As a result, some Sn4+ ions are replaced by Ti4+, leading to structural changes that affect the diffraction pattern [19].

Fig. 1. (a) XRD pattern of TiO2, Sn2+-SnO2, and Sn2+-SnO2/TiO2 and (b) zoomed XRD pattern of Sn2+-SnO2 and Sn2+-SnO2/TiO2 at 2θ of 30–60°.

Table 1. Photocatalytic performance comparison.

| Photocatalyst | Light source | Water Pollutant | Degradation rate (%) | Time (min) | Kinetic constant (min-1) | R2 (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Sn2+-SnO2 (50 mg) | Solar simulator 100 mW/cm2, λ ≥ 450 nm | MO, 16 ppm, 50 mL | 100 | 60 | 0.050 | 96.48 | This work |
|  |  | Cr(VI), 40 ppm, 50 mL | 84.2 | 60 | 0.027 | 99.52 | This work |
| Sn2+-SnO2/TiO2 (50 mg) | Solar simulator 100 mW/cm2, λ ≥ 450 nm | MO, 16 ppm, 50 mL | 100 | 20 | 0.192 | 92.58 | This work |
|  |  | Cr(VI), 40 ppm, 50 mL | 97.9 | 60 | 0.059 | 97.78 | This work |
| Multilayered TiO2@SnO2 hollow nanostructures (100 mg) | UV, Hg lamp, 350 W | MO, 30 ppm, 200 mL | Nearly 85% | 160 | - | - | [20] |
| SnO2 QDs/TiO2 (100 mg) | Xe lamp, 350 W | MO, 10 ppm, 100 mL | 99.3 | 15 | 0.487 | - | [21] |
| Black SnO2–TiO2 composite (25 mg) | Xe lamp, 500 W | MO, 10 ppm, 50 mL | 94.7 | 25 | - | - | [17] |
| SnO2/TiO2 (100 mg) | UV-A, 365 nm, 250 W | Cr(VI), 10 ppm, 150 mL | 97 | 60 | - | - | [22] |
| Sn2+-SnO2 (20 mg) SnO2 TiO2 anatase | UV-A White light UV-A UV-A | MO, 10 ppm, 30 mL MO, 10 ppm, 30 mL MO, 10 ppm, 30 mL MO, 10 ppm, 30 mL | 97 64 No activity No activity | 12 40 - - | - - - - | - - - - | [23] [23] [23] [23] |
| TiO2 | UV-A, 365 nm, 125 W | Cr(VI), 10 ppm, 100 mL | 79 | 180 | - | - | [24] |

### Effect of pH, dosage, and interferents

A series of experiments was conducted to assess the role of pH, catalyst dosage, and common interferents. Fig. 8a shows how pH affects the photocatalytic degradation of methyl orange by Sn2+-SnO2/TiO2 catalysts. The efficiency was strongly influenced by the pH of the solution, decreasing as pH increased. Complete degradation (100%) occurred at pH below 5, dropped to 50% at pH 7, and was nearly absent at pH 10. This behavior is mainly due to changes in the surface charge of the photocatalysts and the anionic nature of methyl orange. In acidic conditions (pH < 6.25), the catalyst surface is positively charged, which enhances the electrostatic attraction and adsorption of the negatively charged dye molecules [25,26]. At pH 2 and pH 5, about 20% of the dye was removed even in the dark, indicating significant adsorption. However, at pH 7 and pH 10, no notable adsorption occurred. As the pH increases, the catalyst surface becomes less positive or even negatively charged, reducing adsorption due to electrostatic repulsion [2]. Similar trends have been observed with other oxide-based photocatalysts. These results suggest that strong dye–catalyst interactions under acidic conditions are essential for high degradation efficiency, while alkaline conditions weaken these interactions and significantly lower photocatalytic activity [2,25].

# Conclusion

In this study, a Sn2+-SnO2/TiO2 heterostructure was successfully synthesized, and the photocatalyst showed high performance for water pollution treatment. It was found that the combination of Sn2+-SnO2 (3.85 ± 0.85 nm) and TiO2 led to the formation of a photocatalyst with a small band gap and improved charge separation efficiency, as confirmed by comprehensive characterization. The photocatalyst also had a high activity in the degradation of organic pollutants and completely decomposed methyl orange within 10 minutes under simulated solar irradiation. Furthermore, it exhibited a high efficiency in heavy metal removal, reducing Cr(VI) by 100% within 45 minutes. The kinetic study shows that Sn2+-SnO2/TiO2 has a higher rate constant than Sn2+-SnO2, being 3.8 times greater for methyl orange degradation and 2.2 times greater for Cr(VI) ion removal under λ ≥ 450 nm illumination. These results indicate that Sn2+-SnO2/TiO2 has the potential to serve as an effective photocatalyst for environmental protection, and the proposed approach can be utilised for the treatment of organic dyes and heavy metal pollutants in wastewater.

# CRediT authorship contribution statement

Haroki Madani: Writing – original draft, Writing – review & editing, Methodology, Conceptualization, Investigation, Formal analysis, Data curation. Saepurahman: Conceptualization, Formal analysis, Supervision, Project administration, Funding acquisition, Writing – review & editing, Validation.

# Declaration of competing interest

All authors consent to this submission and there are no conflicts of interest.

# Acknowledgement

This research received funding from …

# Data availability

Data will be made available on request.

# References

[1]	F.S. Mustafa, A.A. Oladipo, Rapid degradation of anionic azo dye from water using visible light-enabled binary metal-organic framework, J. Water Process Eng. 64, 105686 (2024).

[2]	A.O. Ifebajo, A.A. Oladipo, M. Gazi, Sun-light driven enhanced azo dye decontamination from aqueous solution by CoO-CuFe2O4 derived from layered double hydroxide, Desalination Water Treat. 177, 423–430 (2020).

[3]	M. Furukawa, D. Iwamoto, K. Inamori, I. Tateishi, H. Katsumata, S. Kaneco, Synthesis of Tungsten-Modified Sn3O4 through the Cetyltrimethylammonium Bromide-Assisted Solvothermal Method for Dye Decolorization under Visible Light Irradiation, Catalysts 13, 1179 (2023).

[4]	Ning Yuan, Energy-Efficient MIL-53(Fe)/Sn3O4 Nanosheet Photocatalysts for Visible-Light Degradation of Toxic Organics in Wastewater, Acs Appl. Nano Mater. (2023).

[5]	Sagar Balgude, Yogesh A. Sethi, Bharat B. Kale, N. R. Munirathnam, Dinesh Amalnerkar, Parag V. Adhyapak, Nanostructured Layered Sn3O4 for Hydrogen Production and Dye Degradation Under Sunlight, RSC Adv. (2016).

[6]	Avishek Banik, Mohammad Shaad Ansari, Mohammad Qureshi, Efficient Energy Harvesting in SnO2-Based Dye-Sensitized Solar Cells Utilizing Nano-Amassed Mesoporous Zinc Oxide Hollow Microspheres as Synergy Boosters, Acs Omega (2018).

[7]	W. Jiang, H.K. Loh, B.Q.L. Low, H. Zhu, J.Q. Low, J.Z. Heng, K.Y. Tang, Z. Li, X.J. Loh, E. Ye, Y. Xiong, Role of Oxygen Vacancy in Metal Oxides for Photocatalytic CO2 Reduction, Appl. Catal. B-Environ. 321, 122079 (2022).

[8]	W.-S. Jang, Y. Jin, Y.-H. Kim, S.-H. Yang, S.J. Kim, J.A. Hong, J. Baik, J. Lee, H. Lee, Y.-M. Kim, Site-selective doping mechanisms for the enhanced photocatalytic activity of tin oxide nanoparticles, Appl. Catal. B Environ. 305, 121083 (2022).

[9]	C.V. Reddy, R.R. Kakarla, J. Shim, R.R. Zairov, T.M. Aminabhavi, Hydrothermally derived Cr-doped SnO2 nanoflakes for enhanced photocatalytic and photoelectrochemical water oxidation performance under visible light irradiation, Environ. Res. 217, 114672 (2023).

[10]	H. Roy, T. Rahman, M.A. Jaman, R. Khan, M. Al-Mamun, S.Z. Islam, M.A. Khaleque, M.I. Hossain, M.Z.H. Khan, M.S. Islam, H.M. Marwani, A. Islam, M.M. Hasan, M.R. Awual, Toxic dye removal, remediation, and mechanism with doped SnO2-based nanocomposite photocatalysts: A critical review, J. Water Process Eng. (2023).

[11]	Y. Wang, N. Su, J. Liu, Y. Lin, J. Wang, X. Guo, Y. Zhang, Z. Qin, J. Liu, C. Zhang, X. Qu, W. Li, C. Fu, J. Wang, Q. Zhang, Enhanced visible-light photocatalytic properties of SnO2 quantum dots by niobium modification, Results Phys. 37, 105515 (2022).

[12]	M. Sun, Y. Su, C. Du, Q. Zhao, Z. Liu, Self-doping for visible light photocatalytic purposes: construction of SiO2/SnO2/SnO2:Sn2+ nanostructures with tunable optical and photocatalytic performance, RSC Adv 4, 30820–30827 (2014).

[13]	C.-M. Fan, Y. Peng, Q. Zhu, L. Lin, R.-X. Wang, A.-W. Xu, Synproportionation Reaction for the Fabrication of Sn2+ Self-Doped SnO2-x Nanocrystals with Tunable Band Structure and Highly Efficient Visible Light Photocatalytic Activity, J. Phys. Chem. C 117, 24157–24166 (2013).

[14]	Y. Ding, S. Maitra, C. Wang, S. Halder, R. Zheng, T. Barakat, S. Roy, L.-H. Chen, B.-L. Su, Vacancy defect engineering in semiconductors for solar light‐driven environmental remediation and sustainable energy production, Interdiscip. Mater. 1, 213–255 (2022).

[15]	J. Gupta, P.N.A. Hassan, K.C. Barick, Defects in nanomaterials for visible light photocatalysis, in: 2022: pp. 319–350.

[16]	J. Yin, X. Li, G. Wang, D. Kong, C. Li, D. Xie, Y. Yan, N. Li, Q. Li, (Sn, Ti)O2 solid solution: Mechanically reinforced SnO2@TiO2@C anode for cycle stability of lithium-ion batteries, Electrochimica Acta 507, 145073 (2024).

[17]	J. Yang, J. Zhang, B. Zou, H. Zhang, J. Wang, U. Schubert, Y. Rui, Black SnO2–TiO2 Nanocomposites with High Dispersion for Photocatalytic and Photovoltalic Applications, ACS Appl. Nano Mater. 3, 4265–4273 (2020).

[18]	M. Hirano, T. Kono, Synthesis of Rutile-Type TiO2-SnO2 Solid Solution Nanoparticles by “Forced Co-Hydrolysis” under Hydrothermal Conditions, IOP Conf. Ser. Mater. Sci. Eng. 18, 062015 (2011).

[19]	Francisco Montilla, Emilia MorallÃ3n, A. De Battisti, Alvise Benedetti, Hiromi Yamashita, J.L. VÃ¡zquez, Preparation and Characterization of Antimony-Doped Tin Dioxide Electrodes. Part 2. XRD and EXAFS Characterization, J. Phys. Chem. B 108, 5044–5050 (2004).

[20]	J. Wang, X. Wang, X. Dong, X. Zhang, H. Ma, X. Fei, Multilayered TiO2@SnO2 hollow nanostructures: facile synthesis and enhanced photocatalytic performance, RSC Adv 4, 59503–59507 (2014).

[21]	F. Du, X. Zuo, Q. Yang, B. Yang, G. Li, Z. Ding, M. Wu, Y. Ma, S. Jin, K. Zhu, Facile assembly of TiO2 nanospheres/SnO2 quantum dots composites with excellent photocatalyst activity for the degradation of methyl orange, Ceram. Int. 42, 12778–12782 (2016).

[22]	Y. Zheng, C. Luo, L. Liu, Z. Yang, S. Ren, Y. Cai, J. Xiong, Synthesis of hierarchical TiO2/SnO2 photocatalysts with different morphologies and their application for photocatalytic reduction of Cr(VI), Mater. Lett. 181, 169–172 (2016).

[23]	A. de O. Jorgetto, M.V. Boldrin Zanoni, M.O. Orlandi, Assessment of the superior photocatalytic properties of Sn2+-containing SnO2 microrods on the photodegradation of methyl orange, Sci. Rep. 13, 14774 (2023).

[24]	P. Sane, S. Chaudhari, P. Nemade, S. Sontakke, Photocatalytic reduction of chromium (VI) using combustion synthesized TiO2, J. Environ. Chem. Eng. 6, 68–73 (2018).

[25]	O. Tokode, R. Prabhu, L.A. Lawton, P.K.J. Robertson, The effect of pH on the photonic efficiency of the destruction of methyl orange under controlled periodic illumination with UV-LED sources, Chem. Eng. J. 246, 337–342 (2014).

[26]	N. Bouanimba, N. Laid, R. Zouaghi, T. Sehili, Effect of pH and inorganic salts on the photocatalytic decolorization of methyl orange in the presence of TiO2 P25 and PC500, Desalination Water Treat. 53, 951–963 (2015).